## Slide 1: CORRELATING AND EXTRAPOLATING AIR-PURIFYING RESPIRATOR CARTRIDGE BREAKTHROUGH TIMES –A CRITICAL REVIEW
Gerry O. Wood, PhD
Gerry Odell Consulting
Los Alamos, New Mexico, USA
Anjali Lamba, MPH, CIH
U.S. Environmental Protection Agency

## Slide 2: EPA Need for Guidance
Toxic Substances Control Act (TSCA) of 1976
New Chemicals – Pre-Manufacture Notice
Testing of Cartridges Required
  Use of APRs with Cartridges
  Change-Out Schedule Requirement
Specific submitter case - identified need for updated recommendations for testing and data analysis.

## Slide 3: New EPA Guidance Document

## Slide 4: Companion Document

## Slide 5: Background
Air-Purifying Respirator Cartridges for Gas/Vapor Removal
  Tested for > 100 years
  Data modeled for > 50 years
Cannot test for all possible use conditions
Helpful to be able to extrapolated/interpolate to untested conditions
Most significant use conditions include
  Concentration
  Air flow (breathing) rate
  Humidity
  Temperature
  Interfering covapors or gases

## Slide 6: Objective
Models can be used to interpolate or extrapolate measured breakthrough times for untested conditions.
  Graphs
  Equations
  Rules of Thumb
  Computer programs of complex models
Objective: A critical review of models in the literature.
  New data has been developed over decades
  New understanding of adsorption and chemical removal by impregnants and adsorbed water

## Slide 7: Appendices Outline
Correlations of Breakthrough Times by Empirical Relationships
  Breakthrough curve analysis
  Breakthrough time analysis
  Varying concentration data analysis
  Relative humidity effects analysis
  Temperature effects analysis
  Multiple vapor effects analysis
Extrapolation and Interpolation Using Complex Models and their Derived Computer Programs
  Manufacturers’ programs
  OSHA Advisor Genius
  MultiVapor on NIOSH website
  GasRemove
Evaluations of Rules of Thumb
  Examples from the OSHA website

## Slide 8: Fundamental Breakthrough Time Equation
We W We rB Co – Cb
tb = ------- -- ------- ln ---------- (1)
Co Q kv Co Cb
where We = adsorption capacity (g vapor/ g sorbent)
kv = adsorption rate coefficient (min-1)
W = weight of sorbent (g)
Q = air flow rate (L/min)
rB = packed bed density (g/cm3)
Co = vapor challenge concentration (g/L)
Cb = breakthrough concentration (g/L)
)
)
(
)
(
(

## Slide 9: Correlations of Breakthrough Times for Extrapolations
Analysis | Equations
Breakthrough curve | Curve fitting of Cb or (Cb/Co)vs. t S-shaped curve to Eq. (1) to extract kv and We . Linear plots, ln [Cb / (Co – Cb)] vs. tb is often linear with kv = -Intercept * rB Q / W and We = -(Intercept/Slope) * Co Q / W . Need > 3 data to confirm linearity.
Breakthrough time | Varying sorbent weight or volume for fixed Co and Cb then tb vs. W is often linear with kv = -(Slope/Intercept) * rB Q ln[(Co – Cb)/Cb] and We = Slope * Co Q. Varying air flow rate Q then tb vs. 1/Q is often linear with kv = -(Slope/Intercept) * (rB / W) ln[(Co – Cb)/Cb] and We = Slope * Co / W. Varying bed residence time tR = (VB / Q) (60 sec/min) (1 L / 1000 cm3) by varying bed volume VB and/or Q then tb vs. tR is often linear with kv = -(Slope/Intercept) * ln[(Co – Cb)/Cb] and We = Slope * Co / rB
Varying concentration | Linear plots of log tb vs. log Co for physically adsorbed vapors have been reported, so tb = 10Intercept * CoSlope and We = We1 * CoSlope+1.
Relative humidity effects | Linear functions of RH to a power have been observed: tb(dry) / tb(wet) = 1 + Slope * (RH)n
Temperature effects | Linear plots of tb vs. temperature T (oC) have been reported: tb = tb(reference T) + Slope * T
Multiple vapor effects | Molar additivity method: For an adsorbed vapor x with measured or estimated single vapor breakthrough time tbx, replace Co with Co = Cx + S (Cy­) where Cx is the molar (ppm) concentration of the vapor with the shortest breakthrough time and S Cy is the sum of the molar concentrations of the covapors. Mole fraction method: For an adsorbed vapor x with single vapor capacity Weo and single vapor breakthrough time tbo, use We = [Cx / (Cx + S Cy)] Weo and tb = [Cx / (Cx + S Cy)] tbo
Complex models and computer programs | Breakthrough time estimation model (Wood, 1994). MultiVapor (NIOSH website) GasRemove (GerryOWood.com)

## Slide 11
Nelson, G.O. and C.A. Harder: “Respirator Cartridge Efficiency Studies VI. Effect of Concentration,” Am. Ind. Hyg. Assoc. J. 37:205-216 (1976).
100.67 = 4.7
Reality: Range: 100.395 = 2.5 to 100.937 = 8.6
OSHA Rule of Thumb:
“Reducing concentration by a factor of 10 will increase service life by a factor of 5.”

## Slide 12
Reality: Range: 100.108 = 1.3
to 101.040 = 11.0
OSHA Rule of Thumb:
“Reducing concentration by a factor of 10 will increase service life by a factor of 5.”
Nelson, G.O., G.J. Carlson, and J.S. Johnson: “Service Life of Respirator Cartridges at Various Concentrations of Common Organic Solvents,” Report UCRL-52982, Lawrence Livermore Laboratory, Livermore, CA (1980).

## Slide 13
Reality:
RH effect begins below 85% RH.
Reduction can be much more than 50% and it varies with chemical and carbon.
OSHA Rule of Thumb:
“Humidity above 85% will reduce service life by 50%.”

## Slide 14: OSHA Rule of Thumb: “If the chemical’s boiling point is > 70 oC and the concentration is less than 200 ppm you can expect a service life of 8 hours at a normal work load.”
Chemical | Boiling Point (oC) | Flow (breathing) Rate (L/min) | Concentration (ppm) | Breakthrough Time (hours)
Benzene | 80.1 | 53.3 | 125 | 5.9
Nelson, G.O. and A.N. Correia: “Respirator Cartridge Efficiency Studies: VIII. Summary and Conclusions,” Amer. Ind. Hyg. Assoc. J. 37, 514-525 (1976).

## Slide 15
X
X
X

## Slide 16: Career publications and documents available at: GerryOWood.com